## Slide 1: ROAD MAINTENANCE FORUM 07 April 2022
Presented by
Johan Hattingh

## Slide 2: BASE LAYER MATERIAL FOR PATCHING
Introduction: (Pothole patching as “self-imposed KPI”; Basic pavement management principles must be in-place)
Basic Principles prior to Patching
  Understand or determine mechanism of failure (deformation, binder properties, raveling, crack activity, pumping and poor drainage)
  Design the patch in accordance with the findings of 2i) regarding thickness of repair, follow-up activity, choice of patching materials, related activities, reinstatement of drainage etc.

## Slide 3: BASE LAYER MATERIAL FOR PATCHING
  Choice of Materials for Patching
    Basic Principle: Material to be compatible with existing pavement
      Granular base with granular material of similar properties
      Macadam base with macadam material
      Cemented base with cemented material
      Emergency patching: asphaltic materials (refer to Herman Marias’s presentation)

## Slide 4: BASE LAYER MATERIAL FOR PATCHING
  Basic Construction Techniques
  Limit the depth of sawcut joint to 5mm (Rather, do not use diamond cutting blades)
  Avoid jointing in wheel tracks
  Consider final level of patch with next activity
  Avoid vertical excavation walls (rather step or incline)
  Avoid “dam wall” formation (reservoir effect)

## Slide 5: BASE LAYER MATERIAL FOR PATCHING
  Example of well-intended, but poorly executed pothole patching
  Incorrect choice of base material & poor joint placement

## Slide 6: BASE LAYER MATERIAL FOR PATCHING
  Example of well-intended, but poorly executed pothole patching
  Incorrect choice of base material & poor joint placement

## Slide 7: BASE LAYER MATERIAL FOR PATCHING
  Recent examples of well-intended, but poorly executed pothole patching
  Segregation of G1 aggregate